## Slide 1: Polymers: Essential Background and Definitions

## Slide 2: Contents
Please review the Instructor Document for detailed notes for each slide.
Introduction to polymers (slides 3-6)
Molecular weights and dispersity (slides 7, 8)
Polymer properties (slides 9-11)
Polymer topology (slides 12-13)
Examples of uses/everyday polymers (14-18)

## Slide 3: Polymers Compared to Small Molecules
Rubber
Styrofoam
Polypeptide
Aspirin
Notes: Polymers are depicted as a repeat unit. Shown for comparison is acetyl salicylic acid (aspirin), where the entire molecule is explicitly drawn and all molecules have the exact molecular weight.

## Slide 4: The Repeat Unit
Polymers may have hundreds to thousands of repeat units, making drawing the entire molecule an impossibility.
Polymer chemists take advantage of the repetitive structure, or repeat unit, and draw this:
Segment of poly(vinyl chloride)
Note: End groups are usually omitted, and “n” is often used to show the non-uniformity of chain lengths
Repeat unit of poly(vinyl chloride)
backbone
Pendant group

## Slide 5: Major Classes of Polymers
Vinyl polymers are commonly
used plastics. High molecular
weights are needed to achieve useful
commercial properties
Condensation polymers are commonly
used as fibers, for example in clothing.
Functional groups in the backbone make
these polymers more rigid and useful
at lower molecular weights.

## Slide 6: Polymers are large and slow
Small Molecule Behavior Box
0-500 g/mol
Diffuse easily
Fast mobility
Small
monomer
Polymerization
Large polymer
10,000+ g/mol
Monomers can be liquids or gases
Polymers tend to move slowly than small molecules
Polymers dissolve more slowly in solvents
Polymers possess “memory” of previous shapes
Polyethylene solid
Polystyrene solid
Under ambient conditions:
Ethylene gas
Styrene liquid
Notes: The simplest difference between small molecules and macromolecules is their size, as implied by the terminology. Small molecules are generally no heavier then a few hundred grams per mole, which makes them nimble. Gas molecules bounce around inside their containers and diffuse readily. Liquid molecules engage in vibrant, diffusive, Brownian motion, allowing them to flow even in a condensed phase. Some small molecules possess chemical features that let us use them as monomers. Through polymerization, we convert these individual small monomers into long polymer chains.
In general, a molecular weight of about 10,000 g/mol must be reached for the product to properly behave like a polymer. For reference, you would need to string together about 100 styrene molecules to make a polystyrene chain this heavy. Because the repeat units are now bound to many others in the polymer, the mobility of the structure is greatly reduced. This reduced mobility expresses itself as the polymer having a greater solidity than the monomer, as seen in the lower left representation. The ethylene monomer is a gas, but polyethylene is a dependable solid. Similarly, styrene is a volatile liquid, but polystyrene is a glassy plastic.
This reduced mobility is also responsible for how long it takes polymers to dissolve in a solvent (a week or more!) and how slowly polymers diffuse through a liquid. Finally, the slow polymer chains are similarly slow to respond to deformation, like stretching or compression. They can even get kinetically frozen in a new shape, but still remember a previous one because the chains are so slow to relax and take on new arrangements. If this isn’t handled properly, it can make molded plastic parts break more easily.

## Slide 7: Molecular Weight
All molecules of aspirin (acetylsalicylic acid) have a
molar mass of 180.157 g/mol. This is true regardless of
how or where you synthesized the aspirin.
A sample of polystyrene is made up of molecules
with a variety of molecular weights.
Key point: There is no universal “molecular weight” that applies to all molecules of polystyrene or other synthetic polymers.
Notes: The point of this slide is to differentiate the molecular weight of an organic compound with that of a polymer chain.

## Slide 8: Molecular Weight and Dispersity
A sample of polymer chains will have a variety
of molecular weights. The molecular weight of the
sample is expressed as an “average” molecular weight.
The Dispersity of a polymer sample is a measure of the
extent of this variety.
2 main ways to express the average molecular weight (MW):
Number average MW (Mn) =
Weight average MW (Mw) =
Nx = # of molecules having
a mass of Mx
So, the sample of polymer chains above would have an Mn of 880 g/mol and an Mw of 941 g/mol .
The ratio of these two describes the dispersity of the sample: 1.07 (Mw / Mn)
Notes: This slide gives the details that were introduced in the previous slide.

## Slide 9: Polymers may be semicrystalline
Small Molecule Behavior Box
Well-ordered,
crystalline,
solid
Polymers only partially crystallize in the solid state, resulting in polymer crystallites surrounded by amorphous solid polymer. Some polymers are entirely amorphous and do not crystallize.
Ordered polymer crystallites
Disordered amorphous polymer
Polymer crystals scatter light, making crystalline polymers appear opaque (right) and amorphous polymers appear transparent (left).
Notes: Another key feature of polymers is that they are not entirely crystalline in the solid state. Instead, polymers may be semicrystalline. Small crystallites of ordered polymer are in a sea of disordered, but still solid, polymer. This disordered material is referred to as “amorphous”. The proportion of crystalline to amorphous material depends on the identity of the polymer and exactly how that polymer was processed (for example, how quickly it was cooled from the melt or whether a nucleating agent was added to encourage crystallite growth). Polymers with simple, highly regular structures generally have higher % crystallinity. Branching, long side chains, and low molecular weight all suppress crystallinity. Some polymers are even fully amorphous in the solid state.
The crystallites have melting transitions, just like small molecule crystals, and each polymer has its own particular Tm for the crystalline portion. The amorphous portion has its own thermal transition, the glass transition, which is discussed on the next slide.
Crystallinity has two major effects. More crystalline content provides mechanical reinforcement, resulting in harder, stiffer polymers. Crystallites also scatter light, which results in more crystalline polymers appearing visually opaque. Fully amorphous polymers are visually transparent.

## Slide 10: The Glass Transition (Tg)
Small Molecule Behavior Box
Ordered crystalline solid melts and freezes
H2O (s) ↔ H2O (l)
Tg applies to the amorphous portion of the solid polymer.
Polymer (s, glass) ↔ Polymer (s, rubber)
Each polymer has its own Tg, just like each small molecule has its own Tm.
Temperature
Tg
Above Tg: Polymer is soft and rubbery
Below Tg: Polymer is hard,
brittle, and glassy
Polymer | Tg (°C)
Rayon™ | 157
Polystyrene | 100
PET soda bottle | 69
Teflon™ | -113
Silicone rubber | -123
Plastic trash bag | -125
At
25 °C:
glassy
rubbery
Notes: Conventional small molecules have only one type of solid phase available to them: a well-ordered crystal. However, we saw in the previous slide that polymers are only semicrystalline, at best. The rest of the solid material in a chunk of plastic is “amorphous”. While it is frozen in the solid state (no chains are moving), it doesn’t have any overall order. This is similar to window glass.
Because polymers have two possible solid states, they also have two different solid-phase thermal transitions. Polymer crystallites and small molecules both have melting temperatures, the temperature at which the solid crystal becomes a liquid. The glass transition, however, is unique to polymers, and applies to the amorphous portion of the solid. Below the Tg, the chains are kinetically frozen in place, resulting in brittle, glassy material properties. If the polymer is heated above the Tg, the chains unfreeze and become more mobile. They do not actually melt, but they become flexible rather than frozen. In this state, the polymer shows rubber-like properties like decreased stiffness, stretchability, and bounciness.
Just like each small molecule substance has its own Tm, each type of polymer has its own Tg. The Tg is strongly affected by the structure of the polymer. Things that can increase Tg, and therefore make a polymer glassier, include stiff structures in the backbone like aromatic rings and strong interactions between chains like hydrogen bonding.

## Slide 11: Polymers are viscoelastic
Small Molecule Behavior Box
Under shear (sliding force), a solid stretches like a spring, and a liquid flows. All matter is either solid or liquid, never both.
Polymers are large and therefore slow, so depending on time scale and temperature they may behave -
more like a solid or more like a liquid.
Visco-elastic
“liquid-like”
“solid-like”
Fast Deformation or Low Temperature | Slow Deformation or High Temperature
Reduced chain mobility Fast deformation doesn’t give chains time to relax and flow Low temperatures freeze chains in place Polymer acts more “solid-like” | Increased chain mobility Slow deformation allows chains time to relax and flow High temperatures soften chains, letting them move Polymer acts more “liquid-like”
Notes: Much of what we love about polymers as a material derives from the fact that they simultaneously display solid-like and liquid-like responses to mechanical stress. Ideal liquids and solids consist of a surprisingly tiny portion of the materials we handle every day. Ideal fluids always have the same viscosity, or thickness, no matter how fast you force them to flow. Ideal solids behave like perfect rubber bands; after being stretched or compressed, they return exactly to their previous shape. A classic example of an ideal fluid is air, while the classic ideal solid is a crystal.
Polymers blur the line between these two paradigms, behavior more liquid-like or more solid-like depending on exactly how the deformation is taking place. A ball of silly putty is an excellent visual aid or hands-on manipulative for students to grasp this concept. Silly putty is made of poly(dimethyl siloxane), a common polymer. Because polymer chains have reduced mobility, time-scale is one of the factors that controls the material response. If the polymer is deformed quickly (for example, bouncing silly putty on the table), the chains have no time to react and flow, and therefore the material behaves more like a solid. On the other hand, if you deform the polymer slowly (for example, slowly stretching a silly putty rope), the chains have time to relax and reorganize themselves in response, permitting the material to flow in a more liquid-like manner.

## Slide 12: Topology of Polymers
The properties of synthetic polymers depend not only on their chemical composition, but also on their 3D architecture, or topology. Because polymers are long-chain molecules they can adopt a multitude of conformations which result in different properties.
Examples of polymer topologies are:
Linear
Star
Branched polymer
Cyclic
Graft copolymer
(comb or brush polymer)
Network
(Gel)
Dendrimer

## Slide 13: Topology
Low Density PE-Branched
Plastic wrap, 6 pack rings etc.
High Density PE
(mostly linear)
Bottle Caps, folding chairs etc.
Ultra Molecular weight PE
(long chain)
Parachute cords, body armor, etc

## Slide 14: Familiar Polymers in Everyday Life
PE : plastic grocery bags
PVC : pipes to chewing gum (plasticizer)
Teflon : non-stick coating
Poly(ethylene) (PE)
Poly(vinyl chloride (PVC)
Poly(tetrafluoroethylene)
”Teflon”
Simple changes to the backbone result in major changes in the properties
Notes: (? How do you stick it to the pan)

## Slide 15: Multi-purpose
Windshields (Plexiglass)
Hard contact lens
Cavity fillings
Red “Solo” cups
“Styrofoam”
Poly(methyl methacrylate) (PMMA)
Poly(styrene) PS

## Slide 16: Polymers in Personal Care
Poly(ethylene oxide) (PEO)
Poly(ethylene glycol) (PEG)
Poly(vinyl alcohol) (PVA)
Students : what polymers can you find in your shampoo?
(not the bottle, but the actual ingredients)
Look for :
PVA###
PEG###

## Slide 17: Polymers in Clothing
Vary the R group to control properties
Rayon
Nylon
Poly(ester)
Poly(amide)
Notes: These are often step or condensation polymers.

## Slide 18: Recycling of Synthetic Polymers
Poly(ethylene terephthalate) (PET)
High Density Poly(Ethylene) (HDPE)
Poly(vinyl chloride) (PVC)
Low Density Poly(Ethylene) (LDPE)
Poly(propylene) (PP)
Poly(styrene) (PS)